




TARAVA TEJARAT FARTAK

Applications:R868

High property coating
Production Description:
Inorganic Zr, Al surface coating, organic surface treating Good whiteness, high fluidity and glossiness, good tinting strength, strong hiding power, easy to disperse etc.
Technical data:
	Specification
	Item

	93
	Purity TiO2       ≥

	0.8
	Matter volatile at 105 ˚C % ≤

	0.5
	Hydrotrope %  ≤

	0.05
	Residue on sieve 45 μ m % ≤

	Not lower than
	Color compare with standard

	112
	Tinting strength compare with standard %≥

	7.0-8.8
	PH of suspension, aqueous solution retained

	19
	Oil absorption  g/100g

	50
	Resistivity of aqueous extract Ω m ≥

	97.5
	Rutile crystal form conversion,  %    ≥

	0.3-0.6
	ZrO2    % 

	3.2-4.0
	Al2O3  %

	0.20-0.26
	Average particle diameter μ  m








