TARAVA TEJARAT FARTAK

R868

Applications:

High property coating

Production Description:

Inorganic Zr, Al surface coating, organic surface treating Good whiteness, high fluidity and glossiness, good tinting strength, strong hiding power, easy to disperse etc.

Technical data:

| Specification | Item |
| --- | --- |
| 93 | Purity TiO2 ≥ |
| 0.8 | Matter volatile at 105 ˚C % ≤ |
| 0.5 | Hydrotrope % ≤ |
| 0.05 | Residue on sieve 45 μ m % ≤ |
| Not lower than | Color compare with standard |
| 112 | Tinting strength compare with standard %≥ |
| 7.0-8.8 | PH of suspension, aqueous solution retained |
| 19 | Oil absorption g/100g |
| 50 | Resistivity of aqueous extract Ω m ≥ |
| 97.5 | Rutile crystal form conversion, % ≥ |
| 0.3-0.6 | ZrO2 % |
| 3.2-4.0 | Al2O3 % |
| 0.20-0.26 | Average particle diameter μ m |